## Slide 1
Quantum defects in 2D transition metal dichalcogenides for THz-technologies
Speaker: Jingda Zhang 1,2
Jingda Zhang and Su Ying Quek*
12-Jun-24
1Department of Physics, National University of Singapore, Singapore
2Centre for Advanced 2D Materials, National University of Singapore, Singapore
Notes: https://phys.org/news/2017-05-creation-quantum-emitter-arrays.html

## Slide 2
Spin defects
Isolated point defects:
Atomic-like systems defined by their spin, optical, charge, and their host material
Introducing levels/states in the band gap of semiconductor or insulators
Quantum defects based on electron spin:
Two-level system
Initialization, manipulation, and read-out
Spin-to-charge/photon interfaces
Nat Rev Mater 6, 906–925 (2021).
Notes: Wolfowicz, G. et al. Quantum guidelines for solid-state spin defects. Nat Rev Mater 6, 906–925 (2021).
https://datascience.nih.gov/quantum-information-science.

## Slide 3
NV- centre and more
NV- centre in diamond is a well-established solid-state quantum system.
New-generation defects like defect complexes in SiC or 2D crystals have emerged for scalable quantum technologies.
Electronic structure of NV- centre
Microwave emission by spin defects in SiC
Can we discover the frequency beyond GHz?
Magnetic spin splitting in GHz
Resonance frequency in GHz
Physical Review Applied 9.5 (2018): 054006.
Nanophotonics 8, 1907–1943 (2019).
Notes: Fischer, M., et al. "Highly efficient optical pumping of spin defects in silicon carbide for stimulated microwave emission." Physical Review Applied 9.5 (2018): 054006.
Gali, Á. Ab initio theory of the nitrogen-vacancy center in diamond. Nanophotonics 8, 1907–1943 (2019).

## Slide 4
Terahertz wave:
Important for imaging, sensing, and 6G communications
Technology less mature than other wavelengths
Quantum THz technologies
Single-photon THz emitters:
THz photonic cavity with population inversion
Bring THz communication to additional control in quantum regime
THz spin qubit:
Longer spin relaxation time for robust quantum memory technologies at room temperature
Boost fidelity by resonant optical excitation
THz emission
Optical excitation
J Phys D Appl Phys 50, 043001 (2017).
PRX Quantum 5, 010312 (2024).
Notes: Dhillon, S. S. et al. The 2017 terahertz science and technology roadmap. J Phys D Appl Phys 50, 043001 (2017).
Groiseau, C., Domínguez, A. I. F., Cano, D. M. & Muñoz, C. S. Single-photon source over the terahertz regime. arXiv preprint arXiv:2305.11754 (2023).
Schulte, K. A., Vignesh, K. R. & Dunbar, K. R. Effects of coordination sphere on unusually large zero field splitting and slow magnetic relaxation in trigonally symmetric molecules. Chem Sci 9, 9018–9026 (2018).
Robledo, L. et al. High-fidelity projective read-out of a solid-state spin quantum register. Nature 477, 574–578 (2011).

## Slide 5
Transition metal defects in 2D TMDs
TM substitutional defects:
Heavier elements -> strong spin-orbit coupling (SOC) for large splitting
Magnetism-> high spin state
Multivalences -> both spin and charge degree of freedom
2D transition metal dichalcogenides (TMDs): promising host platform
Thin with easier integration
High light extraction efficiencies
Semiconducting with gate tunability
Scalable and controllable TM incorporation (MOCVD, CVT…)
Appl Phys Rev 7, 031308 (2020).
Nano Res 14, 1668–1681 (2021).
Notes: Ping, Y. & Smart, T. J. Computational design of quantum defects in two-dimensional materials. Nat Comput Sci 1, 646–654 (2021).
Zhang, G., Cheng, Y., Chou, J.-P. & Gali, A. Material platforms for defect qubits and single-photon emitters. Appl Phys Rev 7, 031308 (2020).
Loh, L., Zhang, Z., Bosman, M. & Eda, G. Substitutional doping in 2D transition metal dichalcogenides. Nano Res 14, 1668–1681 (2021).

## Slide 6
First-principles materials discovery
Stability
Spin-triplet
THz-splitting
Excited-states
THz application
Criteria for novel quantum defects
VASP
Density functional theory (DFT):
Charged defects
Spin multiplicity
Single-particle band structures
Zero-field splitting (ZFS) contributed by spin-spin and spin-orbit interactions
Constrained DFT:
Excited-state energies
Group theory analysis
Many-body states
Symmetry-allowed transitions

## Slide 7
Fully-relaxed local atomic structures
Local defect geometries
Symmetry | Displacement vector
D3h | 0
C3v | 
C2v | /
Cs | /
Ch | 
C1 | 
Symmetry | Displacement vector
D3h | 0
C3v | 
C2v | 
Cs | 
Ch | 
C1 | 
C2
σv
C2
σv
σv
C2
C3(S3)
C3(S3)
σh
C2
σyz
σxy
C2
σh
D3h
C2v
Ch
Cs
C1
σs
σs
σyz
Notes: Jingda started with a same C1 symmetry and relaxed for PBE and PBE+U.
For HSE06 relaxations, the starting point is with PBE/PBE+U relaxed structure.

## Slide 8
a
Conduction Band
Ti V Cr Mn Fe Co Ni Cu Zn Zr Nb Ru Rh Pd Ag Cd Hf Ta W Re Os Ir Pt Au Hg
Valence Band
Pink (+1/0);
Green (0/-1);
b
Conduction Band
Ti V Cr Mn Fe Co Ni Cu Zn Zr Nb Mo Ru Rh Pd Ag Cd Hf Ta Re Os Ir Pt Au Hg
Valence Band
0
_
+
0
_
0
0
_
0
_
0
_
0
_
0
_
0
_
0
_
0
_
+
0
+
0
_
+
0
_
+
0
_
0
_
0
_
0
_
0
+
0
+
0
+
0
+
0
_
+
0
_
+
0
_
0
_
+
0
_
0
0
_
0
_
0
_
0
_
0
_
0
_
0
_
0
_
0
+
0
+
0
_
0
_
0
_
0
_
0
_
+
0
+
0
+
0
_
0
_
+
0
_
0
_
0
_
_
Defect charge transition levels
ML MoS2
ML WSe2
represents the charge-dependent finite size FNV correction.
_
Solid (PBE)
Dashed (PBE+U, 3 eV)
Short line:
_

## Slide 9
Spin-triplet quantum defect candidates
TM defect | Charge state | Symmetry | ΔE (Singlet-Triplet) (eV)
Host - MoS2 |  |  | 
Mn | -1 | C2v | 0.69
Fe | 0 | D3h | 0.67
Cu | -1 | C1 | 0.22
Host - WSe2 |  |  | 
Ti | 0 | C2v | 0.01
Mn | -1 | D3h | 0.83
Fe | 0 | D3h | 0.61
Cu | -1 | C1 | 0.08
Cd | 0 | C2v | 0.01
Spin-triplet defect configuration (S = 1) by HSE06

## Slide 10
Zero-field splitting in THz
ZFS lifts the threefold degeneracy of the to be , and and sublevels. The axial and rhombic components of ZFS can be calculated by
x, y, and z are orthogonal electron spin directions assigned in DFT calculations.
The ZFS dominated by SOC is significantly larger than those in other commonly used defects, e.g., NV- centre (~ 3 GHz), and spin defects in SiC and h-BN (< 10 GHz).
Phys Rev X 7, 021046 (2017).
Nat Commun 12, 4480 (2021).
Notes: 1. Christle, D. J. et al. Isolated spin qubits in SiC with a high-fidelity infrared spin-to-photon interface. Phys Rev X 7, 021046 (2017).
2. Gottscholl, A. et al. Spin defects in hBN as promising temperature, pressure and magnetic field quantum sensors. Nat Commun 12, 4480 (2021).

## Slide 11
VB
CB
Electronic structures and many-body level structures of Fe0-MoS2 by HSE06
E-EVBM (eV)
ZPL (Rx, Ry) 0.90 eV
ZFSg
0.3 THz
S = 1
A’1
E”1,2
3A’2
6E”
D3h E 2C3 3C2’ σh 2S3 3σv linear quadratic
A1’ +1 +1 +1 +1 +1 +1 x2+y2, z2
A2’ +1 +1 -1 +1 +1 -1 Rz
E’ +2 -1 0 2 -1 0 (x, y) (x2-y2, xy)
A”1 +1 +1 +1 -1 -1 -1
A”2 +1 +1 -1 -1 -1 +1 z
E” +2 -1 0 -2 +1 0 (Rx, Ry) (xz, yz)
…
…

## Slide 12
VB
CB
E-EVBM (eV)
Electronic structures and many-body level structures of Mn-1-WSe2 by HSE06
D3h E 2C3 3C2’ σh 2S3 3σv linear quadratic
A1’ +1 +1 +1 +1 +1 +1 x2+y2, z2
A2’ +1 +1 -1 +1 +1 -1 Rz
E’ +2 -1 0 2 -1 0 (x, y) (x2-y2, xy)
A”1 +1 +1 +1 -1 -1 -1
A”2 +1 +1 -1 -1 -1 +1 z
E” +2 -1 0 -2 +1 0 (Rx, Ry) (xz, yz)
ZPL (Rx, Ry) 0.58 eV
ZFSg
1.1 THz
S = 1
A’1
E”1,2
3A’2
6E”
…
…

## Slide 13
https://physics.uwo.ca/~mhoude2/courses/PDF%20files/astro9701/Appendix_2.pdf

## Slide 14
Defect state requirements
Mn-1-MoS2/WSe2
Nb-1-WS2
Ti0-WSe2
NV- center: μ = 4.49 D.
The first excitation with valence band (exciton) is optically forbidden.
The next allowed one is between two localized defect states.
The defect transition is symmetry ‘protected’ from detrimental radiative recombinations to band edges states by optical selection rules.
The break of exciton quenches PL at high T.

## Slide 15
Cd0-WSe2
b2
a1
a1
(18.7,50.8,0) D^2
Ti0-WSe2
Mn-1-MoS2
b2
a1
a1
(9.3,6.1,0) D^2
(53.4,36.5,0) D^2
a1
b2
a1

## Slide 16
VB
CB
THz emitter
E-EVBM (eV)
|ZFSg|
3.6 THz
ZPL0/± (x,y) 0.55/0.46 eV
3B2
3A1
A2
Electronic structures and many-body level structures of Ti0-WSe2 by HSE06
B1
A1
18.6 THz
A2
B1
B2
C2v E C2 σv(yz) σv(xy) linear quadratic
A1 +1 +1 +1 +1 y x2, y2, z2
A2 +1 +1 -1 -1 Ry xz
B1 +1 -1 +1 -1 z, Rx yz
B2 +1 -1 -1 +1 x, Rz xy
S = 0
1A1
S = 1

## Slide 17
THz qubit
|ZFSg|
0.05 THz
0.3 THz
ZPL0/± (x,y) 0.61 eV
B1
3B2
3B2
Electronic structures and many-body level structures of Mn-1-MoS2 by HSE06
VB
CB
E-EVBM (eV)
A2
A1
B1
A2
A1
0.3 THz
C2v E C2 σv(yz) σv(xz) linear quadratic
A1 +1 +1 +1 +1 z x2, y2, z2
A2 +1 +1 -1 -1 Rz xy
B1 +1 -1 +1 -1 y, Rx yz
B2 +1 -1 -1 +1 x, Ry xz

## Slide 18
Conceptual design
Outlook for THz quantum defects
The spin state can be read out by the photoluminescence frequency, and the intensity.
ZFS of ground and excited states in THz with opposite signs can boost the fidelity for qubits controlled by resonant excitation.
This study paves the way for breakthroughs in quantum THz technology.
THz emitter
Conduction band
Valence band
Excited state
S=1
Ground state
S = 1
Infrared pumping
THz qubit control

## Slide 19
Acknowledgement
Prof. Su Ying Quek and group
Prof. Goki Eda
Research facilities
Email: jingda@u.nus.edu
Thank you for your attention!

## Slide 20
Computational details
PBE exchange-correlation functional (with an on-site Hubbard U of 3 eV for 3d elements) for preliminary screening and HSE06 functional for further validation
PAW energy cutoff: 450 eV
Supercell of ML TMDs: 4×4 (qualitatively agree with 6×6)
Γ-centred k-mesh: 3×3×1
Force convergence criterion: 0.01 eV/Å for PBE and 0.02 eV/Å for HSE06
Energy convergence criterion in SCF cycle: 10-5 eV
Vacuum height: 15 Å
FNV finite-size correction by sxdefectalign2d code
“LDMATRIX” tag used in SS-contributed ZFS calculations
SOC nonself-consistently included in the SO-contributed ZFS calculations
Optical transition energies by constrained DFT method
PyVaspwfc for post-processing of wavefunction visualization in VESTA
Group theory analysis for configuring many-body states and determining symmetry-allowed transitions

## Slide 21
Zero-field splitting. The first order ZFS contributed by spin-spin dipole interactions is calculated by adding the hidden tag “LDMATRIX” implemented in VASP.
The second-order SOC-contributed ZFS has the spin Hamiltonian of
which yields, for , , , and for , and eigenstates, respectively (see main text).
For a single spin, with the spin-quantization axis in the z-direction, and spin states and , we have
Thus, for two spins in the system,
Therefore, using the Hamiltonian the total energies are:
where is introduced as the total electronic energy, which we assume to be independent of the orientation of the spins. Now, the value of and can be directly calculated by DFT through:
For the calculation of total energies, we first carry out a self-consistent collinear calculation without SOC. Reading from the ground-state charge density of the system, the SOC can be treated as a perturbation in non-self-consistent calculations. The total energy of the system is self-consistently calculated including SOC with a convergence threshold of 10-9 eV for different spin orientations.

## Slide 22
MoS2 | CTL (+1/0) (eV) | CTL (0/-1) (eV)
Ti | -0.40 (-0.39) | 0.67 (0.70)
V | -0.39 (-0.43) | 0.56 (0.65)
Cr | -0.44 (-0.30) | 1.88 (1.48)
Mn | 0.57 (0.30) | 1.55 (1.33)
Fe | 0.39 (0.07) | 1.42 (1.09)
Co | 0.24 (0.07) | 1.20 (1.31)
Ni | 0.08 (0.06) | 1.19 (1.18)
Cu | 0.06 (0.04) | 1.10 (1.08)
Zn | -0.08 (-0.10) | 0.94 (0.92)
Zr | -0.42 | 0.65
Nb | -0.39 | 0.51
Ru | 0.63 | 1.88
Rh | 0.57 | 1.25
Pd | 0.18 | 1.32
Ag | 0.16 | 1.12
Cd | -0.03 | 1.01
Hf | -0.41 | 0.66
Ta | -0.38 | 0.52
W | -0.44 | 2.30
Re | 1.24 | 2.05
Os | 0.73 | 2.02
Ir | 0.79 | 1.30
Pt | 0.22 | 1.34
Au | 0.33 | 1.30
Hg | 0.11 | 1.11
WSe2 | CTL (+1/0) (eV) | CTL (0/-1) (eV)
Ti | -0.43 (-0.41) | 0.43 (0.47)
V | -0.51 (-0.39) | 0.34 (0.48)
Cr | -0.55 (-0.35) | 1.51 (1.17)
Mn | 0.39 (0.16) | 1.24 (0.99)
Fe | 0.26 (-0.08) | 1.22 (0.88)
Co | 0.21 (-0.02) | 0.97 (1.03)
Ni | -0.03 (-0.22) | 0.94 (0.86)
Cu | 0.01 (-0.03) | 0.88 (0.87)
Zn | -0.16 (-0.17) | 0.68 (0.67)
Zr | -0.45 | 0.40
Nb | -0.53 | 0.29
Mo | -0.57 | 1.98
Ru | 0.42 | 1.55
Rh | 0.43 | 0.98
Pd | 0.04 | 1.03
Ag | 0.04 | 0.83
Cd | -0.12 | 0.78
Hf | -0.44 | 0.42
Ta | -0.51 | 0.31
Re | 0.97 | 1.60
Os | 0.48 | 1.68
Ir | 0.55 | 1.06
Pt | 0.05 | 1.04
Au | 0.18 | 1.07
Hg | -0.02 | 0.84

## Slide 23
PBE+U | Charge state | Symmetry | ΔE (Singlet-Triplet) (eV)
Host - MoS2 |  |  | 
Mn | -1 | C2v | 0.60
Fe | 0 | Ch | 0.40
Cu | -1 | Cs | 0.01
Cd | 0 | D3h | 0.03
Hg | 0 | D3h | 0.02
Host - WSe2 |  |  | 
Ti | 0 | C2v | 0.02
Mn | -1 | Ch | 0.81
Fe | 0 | Ch | 0.53
Cu | -1 | Cs | 0.03
Cd | 0 | D3h | 0.02
HSE06 | Symmetry | MAE axis | DSO(GHz) | DSS(GHz) | ESO(GHz) | ESS(GHz) | Dtot(THz)
Host - MoS2 |  |  |  |  |  |  | 
Mn-1 | C2v | ( -1 0) | -52.9 | 19.7 | -9.5 | 10.0 | -0.06
Fe0 | D3h | (0 0 1) | 306.8 | 16.3 | 0.7 | 0.0 | 0.32
Cu-1 | C1 | (0 0 1) | -261.6 | 0.1 | -39.8 | -1.7 | -0.26
Host - WSe2 |  |  |  |  |  |  | 
Ti0 | C2v | (0 0 1) | 3553.7 | 0.9 | -28.7 | 0.1 | 3.55
Mn-1 | D3h | (0 0 1) | -1064.5 | 24.5 | -35.4 | 0.2 | -1.10
Fe0 | D3h | (0 0 1) | 7329.7 | 10.7 | 0.4 | 0.1 | 7.34
Cu-1 | C1 | (0 0 1) | -3670.7 | 0.5 | 12.0 | 1.4 | -3.66
Cd0 | D3h | (0 0 1) | 6822.3 | 0.9 | 1.5 | 0.0 | 6.82
HSE06 | Symmetry | MAE axis | DSO(GHz) | DSS(GHz) | ESO(GHz) | ESS(GHz) | Dtot(THz)
Host - MoS2 |  |  |  |  |  |  | 
Mn-1 | C2v |  | -52.9 | 19.7 | -9.5 | 10.0 | -0.06
Fe0 | D3h | (0 0 1) | 306.8 | 16.3 | 0.7 | 0.0 | 0.32
Cu-1 | C1 | (0 0 1) | -261.6 | 0.1 | -39.8 | -1.7 | -0.26
Host - WSe2 |  |  |  |  |  |  | 
Ti0 | C2v | (0 0 1) | 3553.7 | 0.9 | -28.7 | 0.1 | 3.55
Mn-1 | D3h | (0 0 1) | -1064.5 | 24.5 | -35.4 | 0.2 | -1.10
Fe0 | D3h | (0 0 1) | 7329.7 | 10.7 | 0.4 | 0.1 | 7.34
Cu-1 | C1 | (0 0 1) | -3670.7 | 0.5 | 12.0 | 1.4 | -3.66
Cd0 | D3h | (0 0 1) | 6822.3 | 0.9 | 1.5 | 0.0 | 6.82
PBE+U | Symmetry | MAE axis | DSO(GHz) | DSS(GHz) | ESO(GHz) | ESS(GHz) | Dtot(THz)
Host - MoS2 |  |  |  |  |  |  | 
Mn-1 | C2v | (0 0 1) | -284.8 | 37.8 | -10.6 | 0.9 | -0.25
Fe0 | Ch | (0 0 1) | 409.2 | -8.8 | 0.1 | -0.0 | 0.40
Cu-1 | Cs | (0 0 1) | -145.6 | -2.2 | 0.1 | -0.4 | -0.15
Cd0 | D3h | (0 0 1) | 2797.8 | 1.0 | 0.0 | 0.0 | 2.80
Hg0 | D3h | (0 0 1) | 8255.8 | 1.0 | 0.1 | 0.0 | 8.26
Host - WSe2 |  |  |  |  |  |  | 
Ti0 | C2v | (0 0 1) | -2134.2 | 1.1 | -7.8 | 0.1 | -2.13
Mn-1 | Ch | (0 0 1) | -1892.4 | -23.5 | 50.3 | -0.7 | -1.92
Fe0 | Ch | (0 0 1) | 7431.0 | -5.6 | -0.1 | -0.1 | 7.43
Cu-1 | Cs | ( -1 0) | 491.7 | -1.5 | 9.6 | -0.4 | 0.49
Cd0 | D3h | (0 0 1) | 11638.5 | 0.9 | 0.4 | 0.0 | 11.64
PBE+U | Symmetry | MAE axis | DSO(GHz) | DSS(GHz) | ESO(GHz) | ESS(GHz) | Dtot(THz)
Host - MoS2 |  |  |  |  |  |  | 
Mn-1 | C2v | (0 0 1) | -284.8 | 37.8 | -10.6 | 0.9 | -0.25
Fe0 | Ch | (0 0 1) | 409.2 | -8.8 | 0.1 | -0.0 | 0.40
Cu-1 | Cs | (0 0 1) | -145.6 | -2.2 | 0.1 | -0.4 | -0.15
Cd0 | D3h | (0 0 1) | 2797.8 | 1.0 | 0.0 | 0.0 | 2.80
Hg0 | D3h | (0 0 1) | 8255.8 | 1.0 | 0.1 | 0.0 | 8.26
Host - WSe2 |  |  |  |  |  |  | 
Ti0 | C2v | (0 0 1) | -2134.2 | 1.1 | -7.8 | 0.1 | -2.13
Mn-1 | Ch | (0 0 1) | -1892.4 | -23.5 | 50.3 | -0.7 | -1.92
Fe0 | Ch | (0 0 1) | 7431.0 | -5.6 | -0.1 | -0.1 | 7.43
Cu-1 | Cs |  | 491.7 | -1.5 | 9.6 | -0.4 | 0.49
Cd0 | D3h | (0 0 1) | 11638.5 | 0.9 | 0.4 | 0.0 | 11.64

## Slide 24
Mn-1-WSe2
(0,0,3.6) D^2
(6x6 cell scf by HSE06 relaxed by PBE+U)
(4x4 cell relaxed by HSE06)
(4x4 cell by HSE06+SOC)
mag= -0.0001 -0.0002 2.0213

## Slide 25
Fe0-MoS2
(6x6 cell scf by HSE06 relaxed by PBE+U)
(4x4 cell relaxed by HSE06)
(0,0,2.5) D^2
(4x4 cell by HSE06+SOC)
mag= 0.0000 0.0000 1.9984

## Slide 26
S = 0
S = 1
Fe0-MoS2 by PBE+U
Fe0-MoS2 (S = 0)

## Slide 27
(6x6 cell scf by HSE06 relaxed by PBE+U)
(4x4 cell relaxed by HSE06)
Fe0-WSe2
a”
a”
a’
a’
(0,0,3.3) D^2

## Slide 28
Formation energy of TM defect:
Note that the formation energies are determined with chemical potential under constraint conditions:
Here, M = Mo/W, X = S/Se, TM = Fe/Mn. The boundary for the least limit of formation energy can be derived as:
.
To avoid the uncertainty of values from experiments, we also demonstrate the energy difference between TM forming as substitution or as the interstitial (adsorption above Mo/W or S/Se atom) by PBE+U calculation, which can be expressed by
with
The for Fe0 in MoS2 and Mn0 in WSe2 are is -6.31 eV and -5.90 eV, respectively. This indicates that with the introduction of TM impurities, the formation of substitutional defects is energetically more favourable.
ML WSe2
EXP bandgap~ 1.7 eV
CALC by PBE: 1.54 eV
CALC by HSE06+SOC: 1.62 eV
CALC by HSE06: 1.90 eV
ML MoS2
EXP bandgap~ 1.9 eV
CALC by PBE: 1.68 eV
CALC by HSE06+SOC: 1.97 eV
CALC by HSE06: 2.03 eV

## Slide 29
MoS2 | PBE+U |  |  | HSE06 |  | 
 | Symmetry | ΔE (Singlet-Triplet) (eV) | Triplet dopant position | Symmetry | ΔE (Singlet-Triplet) (eV) | Triplet dopant position
Mn-1 | C2v | 0.60 | 0.328,0.422,0.500 | C2v | 0.69 | 0.328,0.421,0.500
Fe0 | D3h | 0.40 (0.52) | 0.333,0.417,0.501 | D3h | 0.67 | 0.333,0.417,0.500
Cu-1 | Cs | 0.01 (0.06) | 0.315,0.439,0.511 | C1 | 0.22 | 0.316,0.438,0.511
Cd0 | D3h | 0.03 | 0.333,0.417,0.501 |  | 0.00 | 
Hg0 | D3h | 0.02 | 0.333,0.417,0.507 |  | 0.00 | 
Discussion:
HSE06 relaxations start from PBE relaxed structure. The PBE structures with 3d dopants are different from HSE06 relaxed ones, especially for Mn, Fe and Co. However, PBE+U gives much better results. This can be seen from CTLs by PBE+U.
The values in bracket on Sin-Tri gap stand for another S=0 state (defect position closer to triplet). Co-1-WSe2 prefers to form quintet state over triplet (lower by 0.16 eV).
U is set to be 3 eV for 3d dopant elements, performing as a proper correction (also studied in literatures). Linear response is for now not necessary.
WSe2 | PBE+U |  |  | HSE06 |  | 
 | Symmetry | ΔE (Singlet-Triplet) (eV) | Triplet dopant position | Symmetry | ΔE (Singlet-Triplet) (eV) | Triplet dopant position
Ti0 | C2v | 0.02 | 0.332,0.418,0.500 | C2v | 0.01 | 0.331,0.419,0.500
Mn-1 | C2v | 0.81 | 0.327,0.430,0.501 | D3h | 0.83 | 0.333,0.417,0.501
Fe0 | D3h | 0.53 | 0.333,0.417,0.501 | D3h | 0.61 | 0.333,0.417,0.500
Cu-1 | Cs | 0.03 | 0.310,0.441,0.515 | C1 | 0.08 | 0.312,0.440,0.512
Cd0 | D3h | 0.02 | 0.333,0.417,0.501 | C2v(D3h) | 0.01 | 0.333,0.416,0.501

## Slide 30
b
a
Ti
V
Cr
Mn
Fe
Co
Ni
Cu
Zn
Zr
Nb
Mo
Tc
Ru
Rh
Pd
Ag
Cd
Hf
Ta
W
Re
Os
Ir
Pt
Au
Hg
X
Mo/W
S/Se
Trigonal prismatic coordination
C2
σv
C2
σv
σv
C2
C3(S3)
C3(S3)
σh
C2
σyz
σxy
C2
σh
D3h
C2v
Ch
σyz

## Slide 31
a
Conduction Band
Ti V Cr Mn Fe Co Ni Cu Zn Zr Nb Ru Rh Pd Ag Cd Hf Ta W Re Os Ir Pt Au Hg
Valence Band
Pink (+1/0) Green (0/-1)
b
Conduction Band
Ti V Cr Mn Fe Co Ni Cu Zn Zr Nb Mo Ru Rh Pd Ag Cd Hf Ta Re Os Ir Pt Au Hg
Valence Band
0
_
+
0
_
0
0
_
0
_
0
_
0
_
0
_
0
_
0
_
0
_
+
0
+
0
_
+
0
_
+
0
_
0
_
0
_
0
_
0
+
0
+
0
+
0
+
0
_
+
0
_
+
0
_
0
_
+
0
_
0
0
_
0
_
0
_
0
_
0
_
0
_
0
_
0
_
0
+
0
+
0
_
0
_
0
_
0
_
0
_
+
0
+
0
+
0
_
0
_
+
0
_
0
_
0
_
_
ML MoS2
ML WSe2
_
_

## Slide 32
a
Easy-plane anisotropy
b
Easy-axis anisotropy

## Slide 33
THz emission
Near-infrared excitation
Conceptual design for THz emitters for cover page
THz emitter
Conduction band
Valence band
Excited state
S=1
Ground state
S = 1
ZPL
Meta-stable state S=0
ISC
THz qubit control
ISC: Intersystem crossing
ZPL:
Zero-phonon line
ZFS:
Zero-field splitting

## Slide 34
By checking Rh-MoS2(-1) in 6*6 supercell, the same largely distorted geometry occurs, meaning it is not due to the supercell size. Therefore, we need a more reliable method for searching for the real ground state:
Based on the threefold symmetry of substitution site and supposing the a, b, c are unit vectors, the initial geometries choices can be confined in the shaded area.
For C1h/C1, the deviation direction is chosen towards a meta-site Mo/W along bisection angle in between the two C2v movements (0.333,0.417,0.500)->(0.333,0.437,0.520).
Repeat all the calculations from C1 for both S=0 and 1 by PBE:
-> only 2 calculations for each defect charge
-> obtaining CTLs and Sin-Tri gaps within a single batch.
-> energetically more stable configurations than the previous random disruptions for non-constraint spin calculations

## Slide 35
MoS2 | chg | E (new-old eV)
Ti | +1 | 0.02
Zr | +1 | 0.02
Hf | +1 | 0.02
W | -1 | 0.04
Re | 0 | 0.03
Ir | 0 | 0.06
WSe2 | chg | E (new-old eV)
V | 0 | 0.03
V | +1 | 0.03
Cr | +1 | 0.02
Fe | -1 | 0.07
Nb | 0 | 0.04
Mo | -1 | 0.04
Mo | +1 | 0.05
Ta | 0 | 0.03
MoS2 | chg | E (new-old eV)
Co | -1 | -0.10
Ni | 0 | -0.35
Ni | -1 | -0.27
Cu | 0 | -0.09
Cu | -1 | -0.07
Cu | +1 | -0.07
Rh | -1 | -0.30
Pd | -1 | -0.02
Pd | +1 | -0.05
Ag | -1 | -0.07
Ir | -1 | -0.32
Pt | -1 | -0.12
Au | 0 | -0.02
Au | -1 | -0.01
Au | +1 | -0.04
WSe2 | chg | E (new-old eV)
Co | -1 | -0.10
Ni | 0 | -0.36
Ni | -1 | -0.32
Ni | +1 | -0.17
Cu | 0 | -0.13
Cu | -1 | -0.07
Cu | +1 | -0.17
Rh | -1 | -0.26
Ag | -1 | -0.12
Ir | -1 | -0.28
Pt | -1 | -0.10
Au | 0 | -0.09
Au | -1 | -0.04
Au | +1 | -0.07
Comparison of total energy between new and old method
Among 150 systems, 107 systems are very closed by new and old method. Systems with larger than 0.01 eV E_tot difference are listed. The old method do not constrain spin multiplicity.
14 systems (left) show slightly higher energy by new method, probably due to the optimized fractional total magnetic moments by old method. Only 4 systems (bold) may change the CTLs a bit, none of which affect our candidates.
29 systems (right) shows a lower energy by new method. Old method could not even obtain a right spin state (red).

## Slide 36
Application based on ZFS of excited triplet states
In some spectroscopy experiments for organic molecules and theoretical prediction for TM complexes, the ZFS values of excited states can be significantly changed from ground state, even the sign:
J. Phys. Chem. 1992, 96, 6, 2486–2490. (Exp)
J. Phys. Chem. A 1999, 103, 17, 3155–3162. (Exp)
J. Chem. Theory Comput. 2012, 8, 7, 2344–2351. (Calc)
Chem. Sci., 2018, 9, 9018-9026. (Calc)
This occurs obviously in 3d ion doped trigonal crystal field, e.g., ZnGa2O4:Cr3+.
The D component difference between GS and ES can lead to the manipulation of spin Hamiltonian for quantum information process.
2.87 GHz vs 1.43 GHz for NV- centre; Phys. Rev. Lett. 101, 117601.
9.43 GHz vs 2.42 GHz in colour centre in SiC; Nature Physics volume 10, pages157–162 (2014).

## Slide 37
VASP input for step(2)
EDIFF = 1e-9
ICHARG = 11
LCHARG = .FALSE.
LWAVE = .TRUE.
LSORBIT = .TRUE.
SAXIS = 0 0 1/1 1.732 0/1.732 -1 0
Triplet GS
Method1: Tot_E
D_SO
2797.7736486175 GHz
E_SO
-38.0467991705 MHz
Method2: E_soc
D_SO
4698.9114999086 GHz
E_SO
-40.8452999272 MHz
VASP input for step(3)
ISMEAR = -2
EDIFF = 1e-9
ICHARG = 1
LCHARG = .FALSE.
LWAVE = .FALSE.
FERWE = 413*1.0 0.0 1.0 129*0.0 413*1.0 0.0 1.0 129*0.0 413*1.0 0.0 1.0 129*0.0 413*1.0 0.0 1.0 129*0.0 413*1.0 0.0 1.0 129*0.0 413*1.0 0.0 1.0 129*0.0 413*1.0 0.0 1.0 129*0.0 413*1.0 0.0 1.0 129*0.0 413*1.0 0.0 1.0 129*0.0
LDIAG = .FALSE.
LSORBIT = .TRUE.
SAXIS = 0 0 1/1 1.732 0/1.732 -1 0
Triplet ES
Method1: Tot_E
D_SO
-16273.7824136022 GHz
E_SO
3823.0033410819 MHz
Method2: E_soc
D_SO
-18425.1406824871 GHz
E_SO
-359.9019275809 MHz
DFT calculation method:
Triplet GS without SOC
Non-SCF calculations based on three spin orientations
Read previous three WAVECARs for SCF calculations by cDFT, respectively
*The relaxed excited geometry exhibits approximately same ZFS value.
Cd0-MoS2 ZFS of excited state by PBE

## Slide 38
Ir(-1)-WSe2 Band edge (VBM) alignment using core level
PBE
Peak position of pDOS by chalcogen s electrons
0.50 eV = -12.09 + 0 - (-12.59) eV
> 0.48 eV read VBM from the defect band structure
ΔE_VBM_corr = 0.02 eV
0.54 eV = -13.63 + 0 - (-14.17) eV
> 0.44 eV read VBM from the defect band structure
ΔE_VBM_corr = 0.10 eV
HSE06
(Numbers are relative to pri_VBM, respectively)
0.56 eV = -13.91 + 0 - (-14.47) eV
> 0.29 eV read VBM from the defect band structure
ΔE_VBM_corr = 0.26 eV
HSE06soc
0.50 eV = -12.33 + 0 - (-12.83) eV
> 0.39 eV read VBM from the defect band structure
ΔE_VBM_corr = 0.11 eV
PBEsoc
# CTL_1(+1/0)=E_0-(E_p1+FNV_p1)-E_VBM
# CTL_2(0/-1)=-E_0+(E_n1+FNV_n1)-E_VBM
HSE06soc: 1.62 eV gap
CTL_1(+1/0) 0.420
CTL_2(0/-1) 1.383
HSE06: 1.90 eV gap
CTL_1(+1/0) 0.759
CTL_2(0/-1) 1.698
Ir-WSe2 CTLs by HSE06 with and without SOC
Supercell size | 4×4 | 6×6
Defect properties | Ir-1-WSe2 | 
CTL (+1/0) (eV) | 0.552 | 0.438
CTL (0/-1) (eV) | 1.486 | 1.440
Sin-Tri gap (eV) | 0.058 | 0.058
(THz) | 8.694 | 7.914
ZPLT (eV) | 0.439 | 0.456
Supercell size | 4×4 | 6×6
Defect properties | Ir-1-WSe2 | 
CTL (+1/0) (eV) | 0.552 | 0.438
CTL (0/-1) (eV) | 1.486 | 1.440
Sin-Tri gap (eV) | 0.058 | 0.058
 | 8.694 | 7.914
ZPLT (eV) | 0.439 | 0.456
ex’ ey’
a1’
a1’
ex’ ey’
Energy
Character tables
3A’2
A’1
E”1,2
3E’
A”2
A”1
E’x,y
E”1,2
S = 1
S = 0
1A’1
1E’1,2
ZFS
ZPL
D3h
D3h
Ch E σh linear quadratic
A’ +1 +1 x, y, Rz x2, y2, z2, xy
A” +1 -1 z, Rx, Ry xz, yz

## Slide 39
Group theoretic approach for NV- center

## Slide 40
Optical electron spin polarization cycle of NV- center
The nitrogen-vacancy (NV) center has emerged as a versatile atomlike system, finding diverse applications in metrology and quantum information science at room temperature. All of these applications depend critically on a spin-dependent nonradiative transition into a metastable state, the so-called intersystem crossing (ISC), which enables optical initialization and readout of the electronic spin state.
The radiative transitions between the 3A2 and 3E manifolds conserve electronic spin projection, whereas the highly state-selective ISC from the 3E to 1A1 preferentially depopulate A1 and 1E1,2, and the ISC from 1E1,2 to the 3A2 manifold serve to repopulate the ground state for the next optical cycle. The preferential nonradiative depopulation of A1 and E1,2 gives rise to optical spin readout because these states have lower quantum yield. Since the nonradiative repopulation of the 3A2 manifold from 1E1,2 does not appear to be comparably state selective, the preferential nonradiative depopulation of A1 and E1,2 is also predominantly responsible for the optical initialization of the electronic spin into |0>.
Physical review letters, 114(14), 145502.
Physical Review B, 91(16), 165201.
Nanophotonics, 8(11), 1907-1943.
A schematic illustration of the NV center’s level structure. The ISC is responsible for shelving into |1E1,2> via the short-lived |1A1> and for pumping into |0>.
NV center in diamond. (a) Geometry in the core of NV center. (b) Ground-state single particle defect levels in the band gap.
ms=0
ms=±1
~0.4 eV
~0.4 eV
1.19 eV
1.95 eV

## Slide 41
State representation
The single electron orbitals is set by the crystal field and projecting the dangling bonds on each irreducible representation (IR) of the point group of the defect
Dangling bonds representation

## Slide 42
State representation
Two-electron wavefunction transforming as IRs of the group:

## Slide 43
Spin-orbit interaction

## Slide 44
Selection rules
Spin-orbit interaction couples the initial and final states, group theory can decide whether these states are coupled by testing whether the matrix element vanishes by symmetry.
The perturbation does not destroy the symmetry operations and is invariant under all the symmetry operations, must exhibit the full group symmetry, and must therefore transform as the fully symmetric representation . In general case, .
Dresselhaus, M. S., Dresselhaus, G., & Jorio, A. (2007). Group theory: application to the physics of condensed matter. Springer Science & Business Media.

## Slide 45
Spin-orbit coupling matrix and energy diagram